AWG Extruded Tubing Sizes - PTFE, FEP, PFA, ETFE

|  | FEP Applications where FEP tubing is chosen usually require more clarity, flexibility or a lower heat shrinkable temperature than PTFE. |  |  |
| --- | --- | --- | --- |
|  | Inside Diameter (inches) Wall Dimensions (inches) Standard Wall Thin Wall Light weight wall AWG Size Min. Nom. Max Nom. Tol. Nom. Tol. Nom. Tol. Packaging 32 0.008 0.010 0.012 0.005 +/- .002 0.005 +/- .002 - - 1000' Spools 30 0.010 0.012 0.015 0.009 +/- .002 0.009 +/- .002 0.006 +/- .002 1000' Spools 28 0.013 0.015 0.018 0.009 +/- .002 0.009 +/- .002 0.006 +/- .002 1000' Spools 26 0.016 0.018 0.021 0.009 +/- .002 0.009 +/- .002 0.006 +/- .002 1000' Spools 24 0.020 0.022 0.026 0.012 +/- .002 0.010 +/- .003 0.006 +/- .002 1000' Spools 23 0.023 0.026 0.029 0.012 +/- .002 0.010 +/- .003 0.006 +/- .002 1000' Spools 22 0.026 0.028 0.032 0.012 +/- .002 0.010 +/- .003 0.006 +/- .002 1000' Spools 21 0.029 0.032 0.035 0.012 +/- .002 0.010 +/- .003 0.006 +/- .002 1000' Spools 20 0.032 0.034 0.038 0.016 +/- .003 0.012 +/- .003 0.006 +/- .002 1000' Spools 19 0.036 0.038 0.042 0.016 +/- .003 0.012 +/- .003 0.006 +/- .002 1000' Spools 18 0.040 0.042 0.046 0.016 +/- .003 0.012 +/- .003 0.006 +/- .002 1000' Spools 17 0.045 0.047 0.052 0.016 +/- .003 0.012 +/- .003 0.006 +/- .002 1000' Spools 16 0.051 0.053 0.058 0.016 +/- .003 0.012 +/- .003 0.006 +/- .002 1000' Spools 15 0.057 0.059 0.065 0.016 +/- .003 0.012 +/- .003 0.006 +/- .002 1000' Spools 14 0.064 0.066 0.072 0.016 +/- .003 0.012 +/- .003 0.008 +/- .002 500' Spools 13 0.072 0.076 0.081 0.016 +/- .003 0.012 +/- .003 0.008 +/- .002 500' Spools 12 0.081 0.085 0.091 0.016 +/- .003 0.012 +/- .003 0.008 +/- .002 500' Spools 11 0.091 0.095 0.101 0.016 +/- .003 0.012 +/- .003 0.008 +/- .002 500' Spools 10 0.102 0.106 0.112 0.016 +/- .003 0.012 +/- .003 0.008 +/- .002 500' Spools 9 0.114 0.118 0.124 0.020 +/- .004 0.015 +/- .003 0.008 +/- .002 250' Spools 8 0.129 0.133 0.139 0.020 +/- .004 0.015 +/- .003 0.008 +/- .002 - 7 0.144 0.148 0.155 0.020 +/- .004 0.015 +/- .003 0.008 +/- .003 - 6 0.162 0.166 0.174 0.020 +/- .004 0.015 +/- .003 0.010 +/- .003 - 5 0.182 0.186 0.195 0.020 +/- .004 0.015 +/- .003 0.010 +/- .003 - 4 0.204 0.208 0.218 0.020 +/- .004 0.015 +/- .003 0.010 +/- .003 - 3 0.229 0.234 0.244 0.020 +/- .004 0.015 +/- .003 0.010 +/- .003 - 2 0.258 0.263 0.273 0.020 +/- .004 0.015 +/- .003 0.010 +/- .003 - 1 0.289 0.294 0.294 0.020 +/- .004 0.015 +/- .003 0.010 +/- .003 - 0 0.325 0.330 0.342 0.020 +/- .004 0.015 +/- .003 0.012 +/- .003 - |  |