AWG Extruded Tubing Sizes - PTFE, FEP, PFA, ETFE

|  | FEP Applications where FEP tubing is chosen usually require more clarity, flexibility or a lower heat shrinkable temperature than PTFE. |  |  |
| --- | --- | --- | --- |
|  | Inside Diameter (inches); Wall Dimensions (inches). Standard Wall; Thin Wall; Light weight wall. AWG Size; Min.; Nom.; Max; Nom.; Tol.; Nom.; Tol.; Nom.; Tol.; Packaging. 32; 0.008; 0.010; 0.012; 0.005; +/- .002; 0.005; +/- .002; -; -; 1000' Spools. 30; 0.010; 0.012; 0.015; 0.009; +/- .002; 0.009; +/- .002; 0.006; +/- .002; 1000' Spools. 28; 0.013; 0.015; 0.018; 0.009; +/- .002; 0.009; +/- .002; 0.006; +/- .002; 1000' Spools. 26; 0.016; 0.018; 0.021; 0.009; +/- .002; 0.009; +/- .002; 0.006; +/- .002; 1000' Spools. 24; 0.020; 0.022; 0.026; 0.012; +/- .002; 0.010; +/- .003; 0.006; +/- .002; 1000' Spools. 23; 0.023; 0.026; 0.029; 0.012; +/- .002; 0.010; +/- .003; 0.006; +/- .002; 1000' Spools. 22; 0.026; 0.028; 0.032; 0.012; +/- .002; 0.010; +/- .003; 0.006; +/- .002; 1000' Spools. 21; 0.029; 0.032; 0.035; 0.012; +/- .002; 0.010; +/- .003; 0.006; +/- .002; 1000' Spools. 20; 0.032; 0.034; 0.038; 0.016; +/- .003; 0.012; +/- .003; 0.006; +/- .002; 1000' Spools. 19; 0.036; 0.038; 0.042; 0.016; +/- .003; 0.012; +/- .003; 0.006; +/- .002; 1000' Spools. 18; 0.040; 0.042; 0.046; 0.016; +/- .003; 0.012; +/- .003; 0.006; +/- .002; 1000' Spools. 17; 0.045; 0.047; 0.052; 0.016; +/- .003; 0.012; +/- .003; 0.006; +/- .002; 1000' Spools. 16; 0.051; 0.053; 0.058; 0.016; +/- .003; 0.012; +/- .003; 0.006; +/- .002; 1000' Spools. 15; 0.057; 0.059; 0.065; 0.016; +/- .003; 0.012; +/- .003; 0.006; +/- .002; 1000' Spools. 14; 0.064; 0.066; 0.072; 0.016; +/- .003; 0.012; +/- .003; 0.008; +/- .002; 500' Spools. 13; 0.072; 0.076; 0.081; 0.016; +/- .003; 0.012; +/- .003; 0.008; +/- .002; 500' Spools. 12; 0.081; 0.085; 0.091; 0.016; +/- .003; 0.012; +/- .003; 0.008; +/- .002; 500' Spools. 11; 0.091; 0.095; 0.101; 0.016; +/- .003; 0.012; +/- .003; 0.008; +/- .002; 500' Spools. 10; 0.102; 0.106; 0.112; 0.016; +/- .003; 0.012; +/- .003; 0.008; +/- .002; 500' Spools. 9; 0.114; 0.118; 0.124; 0.020; +/- .004; 0.015; +/- .003; 0.008; +/- .002; 250' Spools. 8; 0.129; 0.133; 0.139; 0.020; +/- .004; 0.015; +/- .003; 0.008; +/- .002; -. 7; 0.144; 0.148; 0.155; 0.020; +/- .004; 0.015; +/- .003; 0.008; +/- .003; -. 6; 0.162; 0.166; 0.174; 0.020; +/- .004; 0.015; +/- .003; 0.010; +/- .003; -. 5; 0.182; 0.186; 0.195; 0.020; +/- .004; 0.015; +/- .003; 0.010; +/- .003; -. 4; 0.204; 0.208; 0.218; 0.020; +/- .004; 0.015; +/- .003; 0.010; +/- .003; -. 3; 0.229; 0.234; 0.244; 0.020; +/- .004; 0.015; +/- .003; 0.010; +/- .003; -. 2; 0.258; 0.263; 0.273; 0.020; +/- .004; 0.015; +/- .003; 0.010; +/- .003; -. 1; 0.289; 0.294; 0.294; 0.020; +/- .004; 0.015; +/- .003; 0.010; +/- .003; -. 0; 0.325; 0.330; 0.342; 0.020; +/- .004; 0.015; +/- .003; 0.012; +/- .003; -.. |  |